H81 Series Ink for Silk Screen Printing and Pad Printing

H81:PS.ABS. quick dry, especially rsistance to alcohol, especially wear-resisting, screen printing and pad printing ink

H81 serie ink come out on the base of extensive market researching, customer's universal demand and the development trend of plastic printing,H81 serie ink characteristic is vivid , adapts to the screen printing and pad printing. The ink has the high gloss, especial resistance to alcohol, especial resistance friction, resistant to solvent features, and hardness of ink surface is strong, have very good resistance to scratch and combat . Gorgeous color, enviro nontoxic, accord with EN - 71\1120:2001 European toy safety standards. Suitable for high-end products printing.

Areas of application:

Plastic injection molding, buttons, electrical appliances, membrane switch, wood products, etc.

Application substrate: ABS,PS, change benzene ABS, spray surface of ABS, PVC, PC, acrylic etc.

Ink features:

Super resistance to scratch and smote. This series ink film, ink layer surface hardness obviously are better than similar products, it has strong resistance to scratch and combat .

Testing method:

1,When the ink is completely dry , flat scrape ink layer surface back and forth by nails in a 1000G force,which can not hurt the surface .

2, Especially resistant to alcoholic: this serie ink has excellent resistance to alcohols performance. After dry printing ink layer can effectively resist to various concentrations of dissolution of alcohols such as industrial alcohol, medical alcohol and isopropanol

3,After natural drying 24 hours, in 500G forces, use cotton with alcohol to repeatedly horizontal scrape back and forth on surface, 200 times not dyeing, not losing luster;1000 times not revealing bottom.

4, Special friction resistance: after natural drying 24 hours, in 500G forces, with hard rubber scrapie back and forth on the surface, 3 million times not revealing bottom.

5, Outstanding oil resistance: after the ink complete dry , ink layer is smooth and can resist to white electricity oil, facial cleanser water, anti whitewater, gasoline, oil prebrushing dissolved and corrosion.

6, Excellent printing features: this serie ink never wiredraw in pad printing, design clarity, font and full, edge tidy.

7, Good silk-screen: no plugging edition, especially suitable for fine words, pattern of the printing.

8, weatherproof: be applicable to the outdoor resistance to bask in the product of the printing.

9, Enviro: this serie ink choose pigments not containing heavy metal but environment-friendly materials, products comply correspond with European EN - 71\1122:2001 toy safety standards (heavy metal) test.

Physical features:

Mesh performance:  below the 520 mesh.

Dry time : 8-10min in natural volatility or 2-3min in hot dry

Note:

1, Different material can produce different printing effects, beore using the ink please make small batch test.

2, The test results may change while different test conditions,. The above relevant data for my company laboratory under certain conditions, not as a guarantee that data.

3, This serie of oil ink can not be mixed with other brand.