MICROCOMPUTER WELDING MACHINE USER MANUAL

Microcomputer High Frequency Precision Welding Machine

Operating Manual

www.asc365.com

Directory

One 、 Summarize............................................................................2

Two 、 Technical parameters............................................................2

Three、 Welding current end weld interval .......................................2

Four、  Microprocessor Controller.....................................................3

Five、  Welding current Settings.......................................................3

Six、   How to use help.....................................................................3

Seven、Operating steps......................................................................4

Eight、 General troubleshooting.........................................................4

Nine、  General troubleshootin..........................................................5

One 、Summarize

Microcomputer precise spot welding is according to the current production upscale batteries in the world

（Nickel cadmium, nickel metal hydride, the lithium battery）Needed to specific design。

Single chip microcomputer control，A more stable performance and reliable。My latest product improvement

，Mainly has the following a few big characteristics：

1. Beautiful shape, and lighter。

2. Solder joints and beautiful, the spark small, no black，And steady welding current，Even the size of the solder joints。

3. Completely overcome lithium battery spot welding low voltage and water appears after the phenomenon，Is your battery manufacturing assembly of ideal equipment。

4. Each of the parameters for the digital Settings，So adjust intuitive accurate。

5. The pressure of two welded needle independent regulation，And easy to adjust，Ensure welding stress is stable and reliable。

6. Single chip microcomputer control, double pulse welding。

7. Welding current integral-differential calculation，urrent control is very accurate。

8. Using digital pipe display, keyboard, welding parameters using FLASH storage technology, than previously used code switch out better, don't worry about the code switch with long pull out a code after contact caused by poor welding parameters are not allowed to read。

Two 、Technical Parameters

※Power：AC 110V±10%  50Hz±2Hz

※Output the maximum power： 3KVA

※Welding current：00-99％

※The weight of the：5KG

※Shape dimension：250L×180W×200H（unit：mm）

※Applicable scope：Apply to 0.03 mm to 0.2 mm of various welding pieces。

Three、Welding Current End Eeld Interval

Welding current by users set, welding time by a program for welding time out of calculus, the general welding current are in under 50, welding time in 1-3 ms or so。

Current and time relationship as follows：

| Welding time (%) | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Welding time（ms） | 1.4 | 2.0 | 2.5 | 2.9 | 3.3 | 3.6 | 4.0 | 4.3 | 4.6 | 5.0 |

Four、The Microcomputer Controller

Welding current

indicator

add “↑”

minus “↓ ”

Five、Welding Current Settings

1.  Welding current Settings：

Enter into the normal after welding mode，Direct press "↑" or "press" button to set the need of welding current, shut down after procedures automatically save value。

2.  Indicator that：

Welding long bright lights, not welding flashing lights。

Six、How To Use Help：

1. The power switch: when switch up when the power is connected throw, throw down when cut off power supply  。

2. Work instructions: turn on the power switch, if the lights flashing constantly as normal。

3. Welding current: used to set the size of the current, its configuration range is 00-99; General welding current set in the 25 or so often。

Fuse blocks: 15 A fuse in the electrical box。

4. Welding switch: within the head, when welding needle pressure to welding, closing switches, spot welding to discharge welding, this switch for vulnerable parts。

Seven、Operating Steps：

1、Welding needle height adjustment：

Use first wrench to loosen the welding needle height adjustment screw, and then adjust (or replace) welding show the length of the needle electrode (usually about 15 mm, too long tweldingdeformation needle), to lock the screw 。

2、Electrode (welding needle) width adjustment 。

Use first wrench to loosen the welding needle width adjustment screw, then according to need the width of the welding, adjust the two electrodes make two welding needle to the suitable distance, to lock the screw 。

3、inspection：

Check welding needle for carbon, if there is need file or sand paper to clear it; Then with his right foot pedal and on a ruler to, the nose down, visual welding needle and whether the location for welding on, otherwise, they can be the first step in front of repeat operation, welding and welding required until the position of the needle to it so far。

4、Switch on the power：

First the plug to 220 V power supply socket, and then turn on the power switch, work constantly flickering lights for normal, if the work is not bright or bright lights and no flash, need to shut off the power to restart again。

5、In order to insure good welding quality, must strive continually to trim welding needle, needle with small file will be welding file level off is smooth tips。

Eight、General Troubleshooting

1、Can't make needle or welding electrode contact together, this will make short circuit current, and can't welding。

2、 Adjust current cannot too big, with can live for welding principle, general welding 0.1 mm of welding in 20-30 that can live between welding。

3、There were high pressure case, can't open it。

Nine、General Troubleshooting

| Serial number | Fault phenomena | causes | Elimination method |
| --- | --- | --- | --- |
| 1 | Boot is no power instructions | 1. Insurance tube burned。 2. Input power failure。 | 1.Replace the same specification insurance tube。 2. Overhaul the power lines。 |
| 2 | There are power instructions, no welding sparks | 1. The welding current parameters is too small. 2.Welding switch off the attachment. 3. Start switch damage. 4. Work in bright lights or do not twinkle, mainly is the power to interference。 | 1. Increase the welding current value. 2. Replacement photoelectric switch. 3. Turn off the power switch, turn back on。 |
| 3 | When not firm when welding prison | 1. Check whether to tighten the welding needle 2. Welding joint parts if there's any loose access phenomenon 3. Welding joint parts if there's any loose access control panel and the phenomenon SCR plug is close | To tighten all the parts. |
| 4 | Welding easily when the strike, even burning battery shell | Welding needle end viscosity under a foreign body, Welding materials not. | 1. Increase the welding stress. 2. With small file will end file level off is smooth weld needle. 3. Choose proper welding materials. |

----------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------------

Los Angeles,USA Office Address:426 SOUTH PALM AVENUE  ALHAMBRA，CA 91803  United States  Tel:626-415-6138 Email: hugo@asc365.com

Vancouver,CANADA Office Goldbar Plaza,20800 Westminster Hwy. Unit# 2128, Richmond, BC, V6V 2W3   Canada Tel:778-321-6419 Email:salespacific@asc365.com

Toronto,CANADA Office 2220 Midland Ave. Unit 39-41AP  Scarborough, ON, M1P 3E6  Canada Tel:647-350-2889, 416-727-3877, 416-640-1809  Email: sales@asc365.com