H85 Series of Two-component Metal Glass Ink

H85: low temperature bi-component,（self-desiccation) metal, glass, ceramics, electroplating UV surface, resitant to alcohol, baking 80 ℃, roast 30 minutes.

1,Characteristics:

H85 series is a kind of ink suitable for screen printing, pad printing, light, slow dry solvent-based inks, well printing eligibility, has particularly good adhesion to metal and glass, outstanding performance resistance to dissolve And the drying temperature is low, can effectively conserve energy.

2, Applicable scope:

Suitable for printing metal, glass, partial electroplating materials and some high hardness of spray paint surface.

3, Method of use:

(1) Clearn the surface of the substrate by alcohol or other cleaning liquids .

(2) This product is bi-component reaction type curing inks, before printing according to ink:solid = 100:20 proportion matchs well, agitate, placed after twenty minutes, plus appropriate solvents agitate, then can be printed.

(3) After printing ink layer dry will be somewhat difference because of printing substrate varies , to ensure that quality after printing, please click below form selected dry way and time, the choice of temperature can make the attached to be better and tolerance.

Temperature ℃	80	100	120	150	180
Time

Min	45	30	20	12	8

4, Note:

Before printing please make a test printing, testing the ink whethermatching with Printing materials.

(2) This product is inflammables, before and after using it please completely sealed ink containers and store in cool ventilated place to preserve, avoid contact with high temperature and open flame.

(3) This product has certain excitant to the human body, in use process please get personal protective, avoid contact with skin or drop in eyes, if splashed in eyes by accident, first, please immediately rinse with plenty of water,when necessary, seek medical attention.

(4) Guaranteed quality for one year, overdue please test the usability again.

5, Technical reference see below:

Inspection items	Test results	Test condition
Ink fineness	≤12um	Scraper fineness plan
Dry film burnish	≥80	60 ° mirror surface gloss meters
Drying speed	Surface dry	25 ℃ * 5-10min or 60 ℃ * 2-3min
Entity dry	25 ℃ 48Hr or 80 ℃ * 45min
Resistance to alcoholic	No change	500 grams force/cm2 alcohol cotton 500 times back and forth
Resistance to gasoline	No change	500 grams force/cm2 gasoline cotton 500 times back and forth
Adhesion	100/100	1mm *mm * 100 lattice 3M tape
Resistance to acido	No change	Soak 5% HCI * 24Hr
Resistance to alkaline	No change	Soak 5% 24Hr NaOH *
Resistance to salt	No change	Soak 5% 24Hr NaCl *
Resistance to water	No change	For 20 ℃ tap water * 48Hr
Resistance to heat	No change	80 ℃ * 12H
No change	150 ℃ * 5H
Explain	This series of basic colour and outlets four-color heavy metal content which conform to the European Union ROHS, Europe EN - 71 standards and the United States ASTM standards